## Slide 1: Generalised Halbach Magnets for a Non-Scaling FFAG Arc
Thanks to:
George Mahler – engineering
John Cintorino, Animesh Jain – magnet measurement

## Slide 2: 20-80MeV NS-FFAG Beamline
Parameter | Value | Units
Particle species | Electron | 
Energy range | 20-80 | MeV
Cell Length | 0.251751 | m
Cell Angle | 6.666… | degrees (54 per turn)
R = avg. radius of curvature | 2.16364 | m
Max orbit excursion | 19.83 | mm (from circle radius R)
Tune range per cell | Qy,80 = 0.032, Qx,20 = 0.410 | cycles
Cell lattice | halfD2, QF, D1, BD, halfD2 | 
Drift lengths | D1 = 67.55, D2 = 64.90 | mm
Number of cells | 6 | 
Total length | 1.51051 | m
Total angle | 40 | degrees

## Slide 3: 20, 40, 60, 80MeV in NS-FFAG Cell
1cm grid

## Slide 4: Tunes

## Slide 5: 40 degree NS-FFAG Beamline
10cm grid
6 cells, 12 magnets

## Slide 6: Why am I making this odd thing?
I had some spare Halbach magnets from CBETA prototyping that they’re not using
The 20-80MeV BNL ATF energy range matches the energy range of CBETA magnet halves
  This is by luck, also George Mahler’s idea
It demonstrates 4x energy range in a non-scaling FFAG for the first time (I think)
  Very useful for risk-reduction in the eRHIC design, which uses exactly such FFAGs as transfer lines

## Slide 7: Two Magnet Ideas
Generalised Halbach arrangement
  Vary the size and magnetisation direction of the magnet wedges
  Can produce “any” field configuration
  Or an existing field configuration shifted to better reflect the aperture required by the beams
Permanent magnet shimming with iron wires
  Reduces field errors from “factory” ~1e-2 level to ~1e-4 level for accelerator magnets, cheaply

## Slide 8: Magnet Parameters
Parameter | “QF” magnet | “BD” magnet | Units
Length | 57.44 | 61.86 | mm
Dipole By(x=0) | 0 | -0.37679 | T
Quadrupole dBy/dx | -23.624 | 19.119 | T/m
Inner radius (magnet pieces) | 37.20 | 30.70 | mm
(shim holder) | 34.70 | 27.60 | mm
“Pole-tip” field (magnet pieces) | 0.879 | (-)0.964 | T
Max field at r=1cm | 0.236 | (-)0.568 | T
Outer radius (magnet pieces) | 62.45 | 59.43 | mm
(tubular support) | 76.2 | 76.2 | mm

## Slide 9: Generalised Halbach design
Material grade: N35SH from AllStar Magnetics, Br(eff.)=1.194T
My current sheet approximation code (PM2D) is good enough

## Slide 10: Scaling FFAG example
B0 = 0.2T
R0 = 5m
k = 125
“e-fold length” = R0/k = 40mm
Target GFR = 20mm
Aperture radius = 36.5mm
x (mm) By (T)
-36.5 0.0800
-20 0.1212
0 0.2000
20 0.3294
36.5 0.4965
Max field error = 5.4 Gauss
RMS field error = 0.9 Gauss
Cross-section area = 45.0cm2

## Slide 11: VFFAG example
B0 = 0.2T
k = 25m-1
“e-fold length” = 1/k = 40mm
Target GFR = 20mm
Aperture radius = 36.5mm
y (mm) By (T)
-36.5 0.0803
-20 0.1213
0 0.2000
20 0.3297
36.5 0.4981
Max field error = 3.0 Gauss
RMS field error = 1.0 Gauss
Cross-section area = 43.1cm2

## Slide 12: Photos of magnets (unshimmed)

## Slide 13: 3D Printed Magnet Holder
Field optimiser
 Magnet wedge dimensions
3D print file (.stl mesh)
and block spec. for manufacturer

## Slide 14: Assembly with Dummy Blocks
Old magnet but new ones work the same way

## Slide 15: Rotating Coil
Even older magnet shown here but brass tube is a rotating coil at BNL
Gives multipole field amplitudes at a given radius (R=10mm here)
Stated as fraction of main multipole (quad here) times 10000 to give “units”
<0.5 unit accuracy

## Slide 16: Unshimmed Rotating Coil Results

## Slide 17: Higher Harmonic Figure of Merit
Quadrature sum of units (normal and skew) from sextupole up (10000 units = main quad)
Depends on reference radius
  Small radius: sextupole is dominant
  Large radius: higher order pole contributions increase rapidly

## Slide 18: Figure of Merit vs. Radius

## Slide 19: Iron Wire Shimming Theory
Placing a m=∞ iron cylinder into
a uniform B field distorts the field
lines so they are perpendicular to the surface
Cylinder acquires the surface currents of a cos(q) dipole, giving uniform B and M inside and an external dipole outside
Optimise masses/radii of 32 iron wires placed inside magnet bore to cancel measured errors

## Slide 20: 3D Printed Shim Holder

## Slide 21: Shimming Results (one iteration)
Software error!
No improvement
Re-measured on different sized rotating coil check
Re-aligned the coil, check
One iteration of shimming reduces multipoles by between 3.2x and 6.5x

## Slide 22: Best so far: QF3

## Slide 23: 2nd shimming iteration
Of a previous test quadrupole magnet “5A”
3D printer was worse so had to use clamps for position accuracy!
1 iter  4.4x, 2 iters  15.3x

## Slide 24: Field Strength vs. Spec
Average (integrated) quadrupole for 1st shim iteration:
-19.1142, -19.1176 T/m for BD
goal: 19.1191 T/m
23.6203 to 23.6514 T/m for QF
goal: -23.6236 T/m
Overall sign error because I got the Hall probe the wrong way around during block testing

## Slide 25: Cost and Labour per Magnet
Permanent magnet wedges (AllStar N35SH)
  $1052.67 per QF magnet (16 wedges)
  $758.00 per BD magnet (16 wedges)
Labour ~8h per magnet: 3h measurement, 2h shimming, 2h assembly, 1h 3D printer setup
Required infrastructure
  3D printer ($2-3k), used Ultimaker 2 Extended+
  Rotating coil (~$50k)

## Slide 26: Limitations
Strength
  Upper limit to quad*aperture (pole tip field)
  Watch out for demagnetisation from reverse fluxes (OK so far up to ~1T pole tip)
    Choosing a high Hcj grade increases resistance to this
Can’t have rapidly varying field w.r.t. aperture
Temperature coefficient of NdFeB ~-0.12%/K
Choose high Hcj grade for radiation resistance

## Slide 27: Benefits
No power consumption
  No power supply, no copper wires or windings
Any field shape you like within strength limits
No “cross-talk” between iron surfaces in compact lattices
Can be assembled with mallet
1e-4 accuracy is possible after shimming
Seems cheap, at least for short magnet length

## Slide 28: THE END