## Slide 1: Permanent Magnet VFFA for 18GeV Electron Acceleration

## Slide 2: Status
In Mar/Apr submitted a proposal for BNL lab R&D funding for VFFA design work in 2020-21
  In Oct got negative response (passed 2/3 stages)
But in the preparation of the proposal:
  Built and tuned a prototype VFFA magnet using permanent magnet material
  Searched for VFFA lattice cells for RHIC-sized 18GeV electron machine
  Did 3D tracking of a VFFA test cell

## Slide 3: Project Description
Design and risk-reduce a fixed-field accelerator (likely using permanent magnets) to produce the 18GeV electron bunches for eRHIC instead of an RCS. This eliminates most magnet power supplies and allows a faster acceleration cycle of ≤100 turns, giving a shorter RF pulse and easier spin preservation.
  Cost comparisons showed ~30% cost savings in overall accelerator using eRHIC and CBETA data

## Slide 4: Additional Applications
~mA level electron current could be available at BNL at 18GeV
  Comparable to SLAC
  Can allow beam physics experiments far beyond current ATF reach (70MeV)
Cyclotron-like behaviour at far higher energies
  Flexible time structure
VFFA principle applied to proton machines
  Currently being considered for 1.2GeV neutron source upgrade at RAL
  Forms the basis for waste transmutation “3D cyclotron” facility
    S.J. Brooks, Vertical orbit excursion fixed field alternating gradient accelerators, Phys. Rev. ST Accel. Beams 16, 084001 (2013)

## Slide 5: Arc Lattice Cell Candidates
Estimated dynamic aperture (log)
Magnetic efficiency
0.36T @ 18GeV
0.33T
0.47T
0.57T
0.82T
Field By=B0e-ky
Scaling law means focussing and bending have the same sign
Overall radius and top energy are fixed parameters, vary lattice and amount of reverse bend
Heuristic √bmaxe ≈ 0.1/k
e ≈ 0.01/(k2bmax)

## Slide 6: Full-Scale Lattice Cell

## Slide 7: Demo Magnet Design
k = 20m-1
GFR = 25mm
Bmax = 0.3T
L = 120mm
  5 slices of 24mm
  Using left-over 26x20x24mm blocks from CBETA magnet R&D

## Slide 8: Geometry Optimisation

## Slide 9: 3D Printing from Design

## Slide 10: One-piece assembly doesn’t work: blocks roll around in channel

## Slide 11: Single 24mm-thick Layer

## Slide 12: Slice Repulsion: Need Longer Rods!

## Slide 13: Assembly of Repelling Slices

## Slide 14: Rotating Coil Measurement
3D-printed shim holder

## Slide 15: Harmonics (untuned)

## Slide 16: Harmonics (tuned)

## Slide 17: Field and Error (untuned)

## Slide 18: Field and Error (tuned)

## Slide 19: Gradient and Local k (untuned)

## Slide 20: Gradient and Local k (tuned)

## Slide 21: Extension of Design Height
k = 20m-1
GFR = -25mm to +175mm
Bmax = 0.3T
Max field error ~3 Gauss

## Slide 22: Demo Straight Section (1-72MeV)

## Slide 23: 4×4 Transfer Matrix
Usual (x,x’,y,y’) basis

## Slide 24: Demo Straight Cell Tunes, Height

## Slide 25: Demo Straight Cell Input Steering

## Slide 26: Bent Demo Cell Attempt

## Slide 27: Bent Cell Tunes, Height

## Slide 28: Bent Cell Input Steering

## Slide 29: Bent Cell Input Optical Functions

## Slide 30: Conclusion
VFFAs with permanent magnets are very well suited for high-energy electron machines
  Fields are low to avoid synchrotron radiation, means permanent magnets are applicable
  Beams are small, so dynamic aperture in the VFFA is not a bad constraint, so magnets can be reasonably sized
  Designs even exist where all magnets are below beam synchrotron radiation plane

## Slide 31: BACKUP

## Slide 32: Risks to be Investigated
Simulation:
  Dynamic aperture (non-linear magnetic fields)
  Spin preservation (100 turns is semi-fast acceleration regime)
  Lattice integration (arc-to-straight, linac section)
Experimental:
  Magnet field errors
  Alignment errors after correction (e.g. with piezo movers)
    Before correction is well-known, surveyors can do 100-200um easily
  Verify VFFA and high-phase-advance lattice works in practice (ATF beamline)

## Slide 33: RF, Beam Charge Tradeoffs
200MeV per turn of constant-frequency RF is used, 200MeV injector
If the full 50nC is accelerated in a linac, impedances cause ~3% energy spread, which is too much for the storage ring
Baseline eRHIC uses 5x 10nC bunches to reduce this effect (which is proportional to bunch charge) even when using RCS
Transverse emittance also increases with bunch charge
  Early estimates of VFFA dynamic aperture and bunch emittance are comparable, so needs more detailed calculation

## Slide 34: References
Fixed-field accelerators
  Acceleration in the linear non-scaling fixed-field alternating-gradient accelerator EMMA, S. Machida et al., Nature Physics 8, 243–247 (2012).
  CBETA website: https://www.classe.cornell.edu/Research/CBETA/WebHome.html
  CBETA Design Report, Cornell-BNL ERL Test Accelerator, G.H. Hoffstaetter et al., https://arxiv.org/abs/1706.04245 [physics.acc-ph] (2017).
  CBETA note 032, The CBETA Fractional Arc Test, Ed. C. Gulliford, https://www.classe.cornell.edu/CBETA_PM/index_notes.html
VFFAs
  Vertical orbit excursion fixed field alternating gradient accelerators, S. Brooks, Phys. Rev. ST-AB 16, 084001 (2013).
  Vertical orbit-excursion Fixed Field Alternating Gradient Accelerators and 3D Cyclotrons, S. Brooks, Proc. IPAC’14 (invited talk)
Permanent Magnets
  Production of Low Cost, High Field Quality Halbach Magnets, S. Brooks et al., Proc. IPAC 2017.
  CBETA note 035, CBETA Halbach Magnet Production Run, S. Brooks
ATF fixed-field experiment
  ATF experiment AE-79 “Test of a Large Energy Acceptance NS-FFAG Arc at the ATF”,
  See also talk: Test of Linear-Field Non-Scaling FFAG Arc with a Wide Energy Range, S. Brooks, FFAG’17 workshop: https://indico.bnl.gov/event/2764/