## Slide 1: Permanent Magnets for Emerging Accelerator Applications
CBETA permanent magnet results
Advanced PM design variants
PMs for PETRA-IV parameters

## Slide 2: What is CBETA?
It’s a 4-turn energy-recovery linac (ERL)
  CW operation with superconducting RF
The return loop uses FFA (fixed-field accelerator) technology with permanent magnets
  Returns energies of 42-150MeV in same pipe
  “Non-scaling FFA” (linear field) focussing
    Small dispersion (few cm), short cell length (~45cm)

## Slide 3: Layout & Parameters
Main linac is a 1.3GHz SCRF module with six 5-cell cavities
±36MeV
6MeV
6MeV
42-150MeV
42,78,114,150MeV
Source
Injector cryomodule
Main linac cryomodule
Beam stop
Diagnostic line
Splitter A
Splitter B
Arc A
Arc B
Transition B
Transition A
Straight

## Slide 4: Fixed-Field Return Arc

## Slide 5: Fixed-Field Return Loop Optics
Beams with 4x rigidity range transmitted through same overall radius of curvature in arcs
Adiabatically merged to zero curvature, separation in straights
Beam cell tune decreases as a function of energy

## Slide 7: Magnet Types and Parameters
Magnet | Dipole (T) | Quad (T/m) | Good field radius (mm) | Aperture radius (mm) | Max field (T) (good region) | Max field (T) (aperture)
QF | 0 | -11.5624 | 25 | 43.1 | 0.2891 | 0.4983
BD | -0.3081 | 11.1475 | 25 | 40.1 | 0.5868 | 0.7551
BDT2 | -0.2543 | 11.1475 | 25 | 44.938 | 0.5330 | 0.7552
BDT1 | -0.1002 | 11.1475 | 25 | 49.085 | 0.3789 | 0.6474
QD | 0 | 11.1434 | 25 | 40.1 | 0.2786 | 0.4469

## Slide 8: Layout and Magnet Counts
Permanent magnet total: 216
QF: 107
BD: 32
BDT2: 20
BDT1: 28
QD: 27
QFH: 1 (half length)
BDH: 1

## Slide 9: Permanent Magnet Design
Halbach design made of NdFeB material
This is a combined dipole+quad
Being measured on rotating coil at BNL
3D printed multipole corrector pack inside
Windowframe corrector coil outside
Temperature stabilised by water (orange hoses)
Stephen Brooks et al., "Permanent magnets for the return loop of the Cornell-Brookhaven energy recovery linac test accelerator", Phys. Rev. Accel. Beams 23, 112401 (2020); doi:10.1103/PhysRevAccelBeams.23.112401

## Slide 10: Combined-Function Magnet
Improvement over nested Halbach dipole and quadrupole (shown below) can be made by taking vector sum of the two layers and implementing as a layer with constant magnetisation magnitude but variable wedge thickness.

## Slide 11: Iron Wire Correction Method
Measure bare magnet harmonics, then calculate lengths of iron wires to be inserted around the aperture
8x reduction in field errors
3D printed slot insert
R&D prototype magnet

## Slide 12
CBETA permanent magnet containing tuning wire insert
Electromagnetic corrector coil outside

## Slide 13
CBETA permanent magnet containing tuning wire insert

## Slide 14: Production and Testing Flow
AllStar
PM wedges
KYMA
assembly
1
3
2
4
BNL
tuning
5
Accept
Helmholtz testing at AllStar, 100% of blocks but not temperature controlled
Temperature-controlled Helmholtz test of ~15% sample at BNL for verification
Remainder of blocks shipped directly to KYMA, who also re-test ~10% sample
Rotating coil measurement of bare magnet at BNL
Rotating coil measurement of tuned magnet at BNL

## Slide 15
Permanent magnets shipped from KYMA

## Slide 16
Rotating coil magnet measurement at BNL

## Slide 17
Wire tuning packs for CBETA magnets

## Slide 18
Rotating coil magnet measurement at BNL

## Slide 19
100% complete (excl. spares*)
215 / 215 magnets (0 remaining)
* We have 4 “spare” QFs, 2 BDs for replacing first girder magnets, plus two spare BDT2 magnets, with more spares to be delivered from KYMA

## Slide 20
Permanent magnet total: 216
QF: 107
BD: 32
BDT2: 20
BDT1: 28
QD: 27
QFH: 1 (half length)
BDH: 1

## Slide 21: Final Measurement Rate
Main Production | 
Magnets tuned | 200 (excl. early samples)
Rotating coil measurements | 545
Start date | July 9, 2018
End date | November 14, 2018
Total weeks | 18.2
Magnets tuned per week (avg.) | 10.96
Rotating coil meas. per week (avg.) | 29.88
Rotating coil meas. per magnet (avg.) | 2.73

## Slide 22: Tuned Field Quality Criteria
Unit = 10-4 of main pole
FOM is sqrt(sum of all (multipoles in units)2)
  CBETA FOM is weighted version based on tracking
Midplane error generally hardest to achieve
  May go in and out of spec slightly (~0.5G) due to chiller cycle

## Slide 23: Example Harmonics (QD 2412)

## Slide 24
Only tuned magnets shown (2 “rejects” removed)
Tuned with 96 shims
80 shims
Reject matched with good half
Reject matched with good half
BD
QF
QD
BDT2
QFH
BDT1

## Slide 25: Effect of Tuning (CBETA FOM)
10× improvement

## Slide 26
Only tuned magnets shown (2 “rejects” removed)

## Slide 27
Only tuned magnets shown (2 “rejects” removed)
BD
QF
QD
BDT2
QFH
BDT1

## Slide 28: Water Cooling Stability

## Slide 29: Commissioning results: orbit correction in fixed-field loop
The very first beam through the fixed-field loop on May 7, 2019
Corrected beam using section-by-section local SVD (did not converge for whole FFA)
(June 12, 2019)

## Slide 30: Eventually got 7-turn ERL operation with turns 1,2,3 SVD corrected

## Slide 31
Project | Higher field | Smaller aperture | Open midplane | Oval aperture
Hadron therapy gantry | Yes | Yes | No | Yes
CEBAF 20GeV upgrade | Yes | Yes | Yes | No?
Next-gen light sources | Yes | Yes | Yes | No?
High-gradient quad for capture of laser/plasma accelerator beams | Yes | Yes | No? | Maybe
ERL LHeC | Yes | Yes? | Yes | No?
ILC damping ring | No | No | Yes | No
Demagnetisation?
Radiation resistance?
Assembly precision?
Field quality?
Shimming method?
Novel Permanent Magnet Applications Matrix

## Slide 32: High-Gradient Magnet Proposals
Magnet | Dipole at x=0 (T) | Gradient (T/m) | Beam half-excursion (mm) | Aperture radius (mm)
Therapy gantry | 2020 design by Trbojevic |  |  | 
QF | 0 | 155 | 8.8 | 13.8
BD | 1.8 | -97 | 7.5 | 12.5
Light source | 2019 PRAB publication “Complex Bend II: A new optics solution” |  |  | 
CBII-F | 0.26 | 250 | <0.5 | 5
CBII-D | 0.49 | -250 | <0.5 | 5
All magnets are small aperture, >~100T/m
  Also of interest for focussing in plasma accelerators
3 of 4 have nonzero dipole at nominal beam location

## Slide 33: Trbojevic Hadron Therapy Gantry
A fixed-field gantry transports protons over the wide energy range 65-250MeV to the patient
  Faster depth (energy) scanning because no magnet ramp
  Also lighter-weight and less power than electromagnets
Requires a horizontal beam excursion
  Magnified trajectories shown on right
Higher fields give a smaller rotating gantry

## Slide 34: Next Generation Light Source
A section of alternating, high gradient quadrupoles called a “Complex Bend” reduces the electron beam equilibrium emittance
  This is being considered for the NSLS-II upgrade
  Beam is offset to give overall dipole bending field
A slot is required for synchrotron radiation to escape
  Careful cancellation of field error harmonics
  Their design shown below

## Slide 35: Oval Aperture Comparison
Therapy gantry QF magnet
155T/m quadrupole
27.6mm horizontal aperture
Br = 1.4T material
<10-4 field midplane accuracy
Left: circular aperture
170.9cm2 of material
Right: oval aperture
10mm vertical height
24.0cm2 of material
Sevenfold reduction in material use by only having aperture in the axis where it is needed
cm grid
Same scale!

## Slide 36: Oval Aperture Magnets
This design technique is beyond what was tested at CBETA
Further design optimisation will be done to make magnet more symmetric and manufacturable
7x less area
Or 35% more gradient

## Slide 37: Open-Midplane Magnets Recent Design Improvements in 2020
Same aperture, same field, same field quality, improvement only by design modifications
-250T/m quadrupole combined with 0.49T dipole for NSLS-IIU light source parameter set
5mm Ø aperture, 2mm Ø good field region
  4mm gap open midplane slot
Br = 1.12T material
Quad symmetric
Non-symmetric
Combined function offset
Horizontal midplane only
H-only + combined function
Left-only midplane

## Slide 38: Open-Midplane Area vs. Quality
20x better field quality, and/or less material used
Light source D magnet

## Slide 39: Open-Midplane Area vs. Quality
Light source F magnet
20x better field quality, and/or less material used

## Slide 40: Adaptations for Small Aperture
Iron wires could be adhered to tape rather than plastic cartridge for reduced aperture use
  Or placed in integrated vacuum chamber grooves
SMD rotating coils won’t fit
  Assess capabilities of other existing field measurement systems at SMD and NSLS-II (rotating wire?)
  Could build smaller coil and either rotate coil or magnet
  Horizontal scans with Hall probe or vibrating wire are possible but accuracy is a question, including positional accuracy

## Slide 41: B-H Curve and Demagnetisation
CBETA material grade N35H
External applied field (m0H)
opposing magnetisation direction
Net field (B)
Magnetisation provided by material (m0M = B − m0H)
Large opposing fields (negative H in the direction of M) can potentially demagnetise parts of the material in higher field magnets. Not observed or expected in CBETA (-H<1.3T). Depends on material grade Hcj value.
Hcj value (demagnetisation point,
varies with temperature)

## Slide 42: Reverse H field in magnets
BD
QF
mu0(H.M/|M|) = mu0*‘scalar H’ colour scale
White: 0 to -0.5T; green -0.5 to -1T; yellow/orange -1T to -1.5T (0.1T stripes)

## Slide 43: Radiation Resistance
A.B. Temnykh, NIM A 587 (2008) 13–19
  Experiment: irradiate PMs  measure field loss
  Data fits empirical law where field loss rate varies exponentially with temperature margin to demagnetisation (Curie) temperature
Dose for 1% field loss in CBETA magnets (cautiously) estimated to be 74kGy
  Set a 1kGy lifetime dose limit for <2e-4 field errors
CBETA note 036
https://www.classe.cornell.edu/CBETA_PM/index_notes.html

## Slide 44: Adjustable Permanent Magnets
The CBETA method of main PM plus corrector coil is generally good for <10% adjustability
For full adjustability, could use mechanically-moving parts such as the ZEPTO quadrupole 
  Ben Shepherd, Daresbury Lab, UK
Or could use lattice with two different PM sections that roll mechanically and produce effective variable fields via their vector sum
  Or installing/removing slices for one-time adjustment

## Slide 45: PETRA-IV Magnet Parameters
Name | Type | Strength | Aperture diameter
PSD1A | Sextupole | 3300 T/m2 | 30mm
PSD1D | Sextupole | 4150 T/m2 | 25mm
PSF2A | Sextupole | 4200 T/m2 | 25mm
PQF1 | Quadrupole | 60 T/m | 25mm
PQD2 | Quadrupole | 70 T/m | 25mm
PQD3 | Quadrupole | 50 T/m | 25mm
PQF6 | Quadrupole | 95 T/m | 25mm
PQF8 | Quadrupole | 92 T/m | 25mm
PDQ1 | Dipole+quad | 0.2861 T + 38.94 T/m | 25mm
PDQ2 | Dipole+quad | 0.1976 T + 25.83 T/m | 25mm
PDL1,2(min) | Dipole | 0.2 T | 25mm
PDL1,2(max) | Dipole | 0.4 T | 25mm
POF | Octupole | 300000 T/m3 | 25mm

## Slide 46: Common Parameters
Good field region R=7.9mm
All except PSD1A want ~5 units error
  PSD1A is OK with ~100 units
CBETA N35EH material with Br=1.15791 T
Try 10mm midplane full gap on all magnets
Add 3mm to aperture radius for shims

## Slide 47: Script
halbacharea name=PSD1A R=18e-3 sext=3300 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791 halfoff=0 removeadjacent=0 wedges=24
halbacharea name=PSD1D R=15.5e-3 sext=4150 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791 halfoff=0 removeadjacent=0 wedges=24
halbacharea name=PSF2A R=15.5e-3 sext=4200 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791 halfoff=0 removeadjacent=0 wedges=24
halbacharea name=PQF1 R=15.5e-3 quad=60 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791
halbacharea name=PQD2 R=15.5e-3 quad=70 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791
halbacharea name=PQD3 R=15.5e-3 quad=50 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791
halbacharea name=PQF6 R=15.5e-3 quad=95 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791 halfoff=0 removeadjacent=0
halbacharea name=PQF8 R=15.5e-3 quad=92 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791 halfoff=0 removeadjacent=0
halbacharea name=PDQ1 R=15.5e-3 dipole=0.2861 quad=38.94 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791
halbacharea name=PDQ2 R=15.5e-3 dipole=0.1976 quad=25.83 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791
halbacharea name=PDLmin R=15.5e-3 dipole=0.2 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791
halbacharea name=PDLmax R=15.5e-3 dipole=0.4 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791
halbacharea name=POF R=15.5e-3 oct=300000 gfr=7.9e-3 ymidplane=5e-3 Br=1.15791 halfoff=0 removeadjacent=0 wedges=32
HalbachArea tool available at https://stephenbrooks.org/ap/halbacharea/

## Slide 48: Dipoles
PDL1,2(min)
0.2 T
2.9 units FOM
PDL1,2(max)
0.4 T
4.9 units FOM
Everything is good here
  Probably could use simpler design with rectangular blocks
cm grid

## Slide 49: Quadrupoles
PQF1
60 T/m
3.0 units FOM
PQD2
70 T/m
2.6 units FOM
PQD3
50 T/m
3.6 units FOM
PQF6
95 T/m
4.5 units FOM
PQF8
92 T/m
4.5 units FOM
Weak quads OK, stronger quads are giant!
  Will try some tweaks later

## Slide 50: Combined Function Dipole+Quads
PDQ1
0.2861 T + 38.94 T/m
3.4 units FOM
PDQ2
0.1976 T + 25.83 T/m
5.1 units FOM
These look good, like CBETA but smaller!
  PDQ2 can probably be made to be in spec with a small amount of optimisation

## Slide 51: Sextupoles
PSD1A
3300 T/m2
(“30mm” Ø)
9.3 units FOM
(<100)
PSD1D
4150 T/m2
13.7 units FOM
PSF2A
4200 T/m2
16.0 units FOM
Although the harmonics could be tidied up, these magnets are clearly suffering from the open midplane location
  Sext, oct have high fields at +/-X extremes, exactly where material has been removed
  Will investigate effect of smaller midplane gaps later

## Slide 52: Octupole
POF
300000 T/m3
250.4 units FOM
This hasn’t really converged, with 2.5% field error
  The open midplane is even more difficult for octupole
  Will investigate effect of smaller midplane gaps later

## Slide 53: Try Smaller Aperture on Quads
4.5 units FOM
4.5 units FOM
PQF6
95 T/m
PQF8
92 T/m
R=15.5mm
R=14.5mm
R=12.5mm
7.1 units FOM
22.1 units FOM
6.8 units FOM
21.8 units FOM
Area gets a bit smaller
Harmonics get worse due to proximity of pieces to good field region
Could probably do better with more wedges
Might try reducing midplane instead
Or maybe stronger material grade
Or longer quad in lattice with lower gradient

## Slide 54: Smaller Midplane on Quads
4.5 units FOM
4.5 units FOM
PQF6
95 T/m
PQF8
92 T/m
10mm gap
8mm gap
2.4 units FOM
6mm gap
0.8 units
4mm gap
0.3 units
Design responds well to smaller midplane gap
Area gets considerably smaller
Harmonics get better
This has to be weighed against any practical issues of having such a small midplane gap
2.3 units FOM
0.7 units
0.3 units

## Slide 55: Smaller Midplane on Sextupoles
PSD1A
3300 T/m2
(“30mm” Ø)
PSD1D
4150 T/m2
PSF2A
4200 T/m2
9.3 units FOM
(<100)
13.7 units FOM
13.7 units FOM
10mm gap
8mm gap
6mm gap
4mm gap
2.3 units FOM
1.0 units
0.5 units
Maybe not allowed due to 10mm pole gap required in spec?
Magnets respond well to smaller midplane gap, improving field quality and greatly reducing area.
6.2 units FOM
1.5 units
0.5 units
6.5 units FOM
1.6 units
0.5 units

## Slide 56: Try Smaller Midplane on Octupole
10mm gap
8mm gap
6mm gap
4mm gap
POF
300000 T/m3
250.4 units FOM
59.2 units FOM
(weird convergence?)
5.8 units FOM
0.8 units
Rapid improvement of accuracy and area with smaller midplane gap
Seems to be a threshold for it to become “good”
A different magnet block geometry (i.e. not radial wedges) might give better results in marginal cases

## Slide 57: PETRA-IV Magnets Conclusions
Many of these magnets can be implemented as permanent magnets with open midplanes
  Some look quite compact and/or similar to CBETA
In the more difficult cases, field quality and size depend on the midplane gap required
These designs assume fixed field strength
  Adjustable fields (particularly over a wide range) require different design approaches

## Slide 58: Overall Conclusions, Future Work
Successful implementation of permanent magnets with new features in CBETA
  “Accelerator quality” field in Halbach-style magnet
  Flexible: combined function magnets possible
  Compact and relatively cheap, no power supply
Currently applying for BNL lab funding to investigate smaller, higher-gradient, open-midplane and/or oval PMs
  Further extends PM accelerator applications

## Slide 59: References
A. Bartnik et al., "CBETA: First Multipass Superconducting Linear Accelerator with Energy Recovery", Phys. Rev. Lett. 125, 044803 (July 2020)
Stephen Brooks et al., "Permanent magnets for the return loop of the Cornell-Brookhaven energy recovery linac test accelerator", Phys. Rev. Accel. Beams 23, 112401 (2020); doi:10.1103/PhysRevAccelBeams.23.112401
Dejan Trbojevic et al., "Permanent Halbach Magnet Proton and Superconducting Carbon Cancer Therapy Gantries" Proc. IPAC2017; doi:10.18429/JACoW-IPAC2017-THPVA094 available from http://jacow.org/ipac2017/papers/thpva094.pdf
Amin Ghaith et al., "Permanent Magnet-Based Quadrupoles for Plasma Acceleration Sources", Instruments 2019, 3, 27; doi:10.3390/instruments3020027
Stephen Brooks, CBETA note 035 "CBETA Halbach Magnet Production Run", available from https://www.classe.cornell.edu/CBETA_PM/index_notes.html
Stephen Brooks et al., "Production of Low Cost, High Field Quality Halbach Magnets", Proc. IPAC2017, pp. 4118-4120; doi:10.18429/JACoW-IPAC2017-THPIK007 available from http://jacow.org/ipac2017/papers/thpik007.pdf

## Slide 60: BACKUP

## Slide 61: Rejects/Repaired
BD 2305
Harmonics simulation w/swap
QF 2509
Harmonics simulation w/swap
QD 2427
Harmonics sim. w/type change
QF 2572
Harmonics sim. w/type change

## Slide 62: Reversed Block in QF 2509

## Slide 63
CBETA windowframe correctors at BNL

## Slide 64
CBETA girder production at BNL

## Slide 65
CBETA first FFA girder at BNL
Half-length magnet for matching

## Slide 66
CBETA first FFA girder under construction at BNL

## Slide 67: Other Problems/Lessons Learned
@BNL
  Warehouse roof leaks, hence tent in photo
  Gaps when reassembling magnets from halves
@AllStar
  Some blocks went rusty (not passivated?), had them re-made
  One type magnetisation angle was out-of-spec, had them re-made
@KYMA
  Couple of blocks inserted backwards
  One glue failure, exploding magnet, repaired
Team effort
  Block width with chamfer was not communicated clearly to AllStar, meaning blocks slightly larger than needed, had trouble fitting
  Chinese sign convention for magnetisation was opposite, had to invert blocks

## Slide 68: Helmholtz Measurements
Example: AllStar data for wedge types P1 through P16 (BD magnet)
Angle errors Strength variation

## Slide 69: Magnetisation Angle Distributions
Requested that factory re-make types P15 and P16 to reduce systematic error.
These are the smallest blocks, so not critical, but re-make will improve quality of untuned magnets.
General request was for 1 degree RMS error, but can cope with some above and some below as we have here (see next slide)

## Slide 70: Magnet Error Model
Both the strength and angle error distribution can be put back into the field simulation
Example: BD magnet using AllStar’s data set.
1000 magnets were generated, some with position errors. Histogram is binned by the “units FOM”.
Green = easy to tune
Red = possible problems
Based on first girder experience.

## Slide 71: One-turn Whole-FFA SVD Correction
This used an FFA response matrix generated semi-empirically from the phase advances of the first two corrector orbit bumps in each plane
(October 24, 2019)

## Slide 72: Two Turns Uncorrected
(October 23, 2019)

## Slide 73: Two Turns Corrected with SVD
(November 8, 2019)

## Slide 74: All Four Tunes Compared to Model

## Slide 75: Closed Orbit Bumps (1-turn)
(November 6, 2019)