## Slide 1: Enhanced Field Quality Halbach Magnets for Particle Accelerators
As produced for the return arc of the CBETA four-turn energy-recovery linac at Cornell University

## Slide 2: What is CBETA?
It’s a 4-turn energy-recovery linac (ERL)
  CW operation with superconducting RF
The return loop uses FFA (fixed-field accelerator) technology with permanent magnets
  Returns energies of 42-150MeV in same pipe
  “Non-scaling FFA” (linear field) focussing
    Small dispersion (few cm), short cell length (~45cm)

## Slide 3: CBETA Energy Saving Technologies
Permanent magnets
Superconducting RF
Energy recovery (6  150  6MeV)
Recirculation: 4x beamline reuse, 4x energy
Funded by NYSERDA from Nov’16 to Apr’20
  (NY State Energy R&D Authority)
  $25M grant
  Cornell already had the injector & cryomodule

## Slide 4: Layout & Parameters
Main linac is a 1.3GHz SCRF module with six 5-cell cavities
±36MeV
6MeV
6MeV
42-150MeV
42,78,114,150MeV
Source
Injector cryomodule
Main linac cryomodule
Beam stop
Diagnostic line
Splitter A
Splitter B
Arc A
Arc B
Transition B
Transition A
Straight

## Slide 5: Fixed-Field Return Arc

## Slide 6: Fixed-Field Return Loop Optics
Beams with 4x rigidity range transmitted through same overall radius of curvature in arcs
Adiabatically merged to zero curvature, separation in straights
Beam cell tune decreases as a function of energy

## Slide 8: Magnet Types and Parameters
Magnet | Dipole (T) | Quad (T/m) | Good field radius (mm) | Aperture radius (mm) | Max field (T) (good region) | Max field (T) (aperture)
QF | 0 | -11.5624 | 25 | 43.1 | 0.2891 | 0.4983
BD | -0.3081 | 11.1475 | 25 | 40.1 | 0.5868 | 0.7551
BDT2 | -0.2543 | 11.1475 | 25 | 44.938 | 0.5330 | 0.7552
BDT1 | -0.1002 | 11.1475 | 25 | 49.085 | 0.3789 | 0.6474
QD | 0 | 11.1434 | 25 | 40.1 | 0.2786 | 0.4469

## Slide 9: Layout and Magnet Counts
Permanent magnet total: 216
QF: 107
BD: 32
BDT2: 20
BDT1: 28
QD: 27
QFH: 1 (half length)
BDH: 1

## Slide 10: Permanent Magnet Design
Halbach design made of NdFeB material
This is a combined dipole+quad
Being measured on rotating coil at BNL
3D printed multipole corrector pack inside
Windowframe corrector coil outside
Temperature stabilised by water (orange hoses)
Stephen Brooks et al., "Permanent magnets for the return loop of the Cornell-Brookhaven energy recovery linac test accelerator", Phys. Rev. Accel. Beams 23, 112401 (2020); doi:10.1103/PhysRevAccelBeams.23.112401

## Slide 11: Combined-Function Magnet
Improvement over nested Halbach dipole and quadrupole (shown below) can be made by taking vector sum* of the two layers and implementing as a layer with constant magnetisation magnitude but variable wedge thickness.
* Not exactly a vector sum, needs numerical optimiser for accurate design

## Slide 12: Error Sources (~10-2 level)
Wedge magnetisation vector
  1-2° angle variation
  ~1% strength variation
  Comes from wedge manufacturing process
Wedge position
  0.1-0.2mm XY displacement
  Angle errors (probably fraction of a degree)
  Comes from magnet assembly

## Slide 13: Iron Rod Correction Method
Measure bare magnet harmonics, then calculate lengths of iron rods to be inserted around the aperture
8x reduction in field errors
3D printed slot insert
R&D prototype magnet

## Slide 14
CBETA permanent magnet containing tuning rod insert
Electromagnetic corrector coil outside

## Slide 15
CBETA permanent magnet containing tuning rod insert

## Slide 16: Field Calculation of Magnet Blocks
Magnetostatics:
Areas of constant magnetisation are equivalent to sheet currents around surfaces:
Field of 2D sheet current js from (0,0) to (a,0):
Rotate, add together for each side of polygon

## Slide 17: Field Calculation of Iron Rods
Field of 2D perfect m=∞ iron rod of circular cross-section, centre (0,0), in ambient field B0:
Rod is magnetised with M=2B0
Brod
B0+Brod

## Slide 18: Overall Philosophy
Optimiser
Simulation
Build
Measure
Optimiser
Correction simulation
Correct
Measure
Optimiser
Simulation
Build
Measure
Direct approach:
Incorporating correction:

## Slide 19: Correction Makes Precision Easier
Optimiser
Simulation
Build
Measure
Optimiser
Correction simulation
Correct
Measure
Optimiser
Simulation
Build
Measure
At ~10-4 accuracy
At ~10-2 accuracy
At ~10-2 of error
Measurement steps still have to be ≤10-4
$$$$
$
$

## Slide 20
Permanent magnets shipped from KYMA

## Slide 21
Rotating coil magnet measurement at BNL

## Slide 22
Rod tuning packs for CBETA magnets
Iron rod optimisation program was packaged so that technicians could run it: rotating coil data  rod lengths

## Slide 23
Rotating coil magnet measurement at BNL

## Slide 24: Tuned Field Quality Criteria
Unit = 10-4 of main pole
FOM is sqrt(sum of all (multipoles in units)2)
  CBETA FOM is weighted version based on tracking
Midplane error generally hardest to achieve
  May go in and out of spec slightly (~0.5G) due to chiller cycle

## Slide 25
Only tuned magnets shown (2 “rejects” removed)
Tuned with 96 shims
80 shims
Reject matched with good half
Reject matched with good half
BD
QF
QD
BDT2
QFH
BDT1

## Slide 26: Effect of Tuning (CBETA FOM)
10× improvement

## Slide 27
Only tuned magnets shown (2 “rejects” removed)

## Slide 28: 250T/m Tiny Quad Design Example
Perfect magnet (mm grid)
1.98 units error
±0.25mm position errors
96.59 units error
Corrected with 16 iron rods
2.51 units error
±0.25mm position errors on rods
31.05 units error
Errors, correction, errors in correction
New size regime  sensitivities are different

## Slide 29: Use of 3D Printing in Prototypes
Field optimiser
 Magnet wedge dimensions
3D print file (.stl mesh)
and block spec. for manufacturer

## Slide 30: Custom and Cheap – is it possible?
Combined function dipole+quad
Design for By = B0rk
Magnet design program generates mesh
3D printed
Material cost: $800

## Slide 31
Magnets built as part of CBETA R&D had iron rods inserted and were used to build an FFA test girder

## Slide 32: FFA Test Girder (18-70MeV)
Apr 7, 2017

## Slide 33: Installed at BNL ATF (Accelerator Test Facility)
ATF experiment AE79
May 1, 2017

## Slide 34: Tracking of (x,x’) Offsets
Trajectories have been magnified transversely by 16x for visibility
xin ±1mm
x’in ±10mrad

## Slide 36: First Beam during Fault Studies
May 4, 2017
54MeV was the first energy to be tested

## Slide 37: With Survey “Faro Arm” Attached
May 5, 2017
Most magnet offsets <0.2mm; RMS 0.1mm or better

## Slide 38: All Energies Phase Advance

## Slide 39: Transfer Matrix XX Element
“Measurement” is just taking the difference of a pair of centroids in the good area of the scan

## Slide 40: Transfer Matrix YY Element

## Slide 41: Simulation Conclusions
Correction scheme simulations can be as important as the original design
  Easy/cost effective path to higher accuracy
  Can be automated, integrated into manufacturing
  Don’t just simulate “errors” and then stop
Empirical retuning of simulation assumptions based on measurements?
  Reality is always slightly different to ideal case

## Slide 42: References
A. Bartnik et al., "CBETA: First Multipass Superconducting Linear Accelerator with Energy Recovery", Phys. Rev. Lett. 125, 044803 (July 2020)
Stephen Brooks et al., "Permanent magnets for the return loop of the Cornell-Brookhaven energy recovery linac test accelerator", Phys. Rev. Accel. Beams 23, 112401 (2020); doi:10.1103/PhysRevAccelBeams.23.112401
Stephen Brooks, CBETA note 035 "CBETA Halbach Magnet Production Run", available from https://www.classe.cornell.edu/CBETA_PM/index_notes.html
Stephen Brooks et al., "Production of Low Cost, High Field Quality Halbach Magnets", Proc. IPAC2017, pp. 4118-4120; doi:10.18429/JACoW-IPAC2017-THPIK007 available from http://jacow.org/ipac2017/papers/thpik007.pdf

## Slide 43: BACKUP

## Slide 44
Only tuned magnets shown (2 “rejects” removed)
BD
QF
QD
BDT2
QFH
BDT1

## Slide 45: Production and Testing Flow
AllStar
PM wedges
KYMA
assembly
1
3
2
4
BNL
tuning
5
Accept
Helmholtz testing at AllStar, 100% of blocks but not temperature controlled
Temperature-controlled Helmholtz test of ~15% sample at BNL for verification
Remainder of blocks shipped directly to KYMA, who also re-test ~10% sample
Rotating coil measurement of bare magnet at BNL
Rotating coil measurement of tuned magnet at BNL

## Slide 46: Helmholtz Measurements
Example: AllStar data for wedge types P1 through P16 (BD magnet)
Angle errors Strength variation

## Slide 47: Magnetisation Angle Distributions
Requested that factory re-make types P15 and P16 to reduce systematic error.
These are the smallest blocks, so not critical, but re-make will improve quality of untuned magnets.
General request was for 1 degree RMS error, but can cope with some above and some below as we have here (see next slide)

## Slide 48: Magnet Error Model
Both the strength and angle error distribution can be put back into the field simulation
Example: BD magnet using AllStar’s data set.
1000 magnets were generated, some with position errors. Histogram is binned by the “units FOM”.
Green = easy to tune
Red = possible problems
Based on first girder experience.

## Slide 49
100% complete (excl. spares*)
215 / 215 magnets (0 remaining)
* We have 4 “spare” QFs, 2 BDs for replacing first girder magnets, plus two spare BDT2 magnets, with more spares to be delivered from KYMA

## Slide 50
Permanent magnet total: 216
QF: 107
BD: 32
BDT2: 20
BDT1: 28
QD: 27
QFH: 1 (half length)
BDH: 1

## Slide 51: Final Measurement Rate
Main Production | 
Magnets tuned | 200 (excl. early samples)
Rotating coil measurements | 545
Start date | July 9, 2018
End date | November 14, 2018
Total weeks | 18.2
Magnets tuned per week (avg.) | 10.96
Rotating coil meas. per week (avg.) | 29.88
Rotating coil meas. per magnet (avg.) | 2.73

## Slide 52: Example Harmonics (QD 2412)

## Slide 53: Water Cooling Stability